CERTIFICATE OF ANALYSIS

FOR

TANTALUM POWDER

| P/O No.: xxx52 LOT No.: HTA 6231xxx | SIZE: -325 mesh QUANTITY: 250 kg |
| --- | --- |

1. CHEMICAL ANALYSIS (% WT)

| C N O H Al Cr Fe Mn | 0.0058 0.0032 0.1300 0.0010 0.0010 0.0012 0.0028 0.0003 | Mo Ni Si Ti W Nb Ta | 0.0012 0.0025 0.0030 0.0005 0.0025 0.0050 REMAINDER |
| --- | --- | --- | --- |

2. SPECIFICATION

| PURITY (Excluding Nb & Gas) PARTICLE SIZE | 99.9% min -325 mesh |
| --- | --- |

WE HEREBY CERTIFY THAT THE ABOVE PRODUCT IS CONFORMING TO THE SPECIFICATIONS, AND THERE IS NO MATERIAL ORIGINATED FROM DRC OR ADJOINING COUNTRIES IN AFRICA.